## Slide 1
synthesis of doped Molybdenum (oxy)nitride or carbide nanocomposites by Laser pyrolysis for electrochemical H2 evolution reaction
P. Lonchambon1, S. Surble1, N. Herlin1
G. Dubois2, P. Badaki1,2, F. Tessier2, C. Lagrost2
F. Grasset3
1 CEA, CNRS, NIMBE, Université Paris-Saclay
2 ISCR UMR6226, Rennes
3 LINK IRL3629, Tsukuba

## Slide 2: Outline
Context :
Synthesis and characterizations : laser pyrolysis method
preliminary HER measurements

## Slide 3: Context : Hydrogen Evolution Reaction
H2 is of major interest for energy transition
A promising strategy for production of “clean H2“ : electrochemical water splitting
Need for the development of efficient catalysts
- the most efficient : Pt
- possible alternatives ? Mo based catalysts

## Slide 4: Context : Hydrogen Evolution Reaction
H2 is of major interest for energy transition
A promising strategy for production of “clean H2“ : electrochemical water splitting
Need for the development of efficient catalysts
- the most efficient : Pt
- possible alternatives ? Mo based catalysts
W. Hua et al., A review and perspective on molybdenum-based electrocatalysts for hydrogen evolution reaction, Rare Met. 2020, 39, 335.
polarization curves
Carbon sheet
Mo based materials
Mo based materials in carbon
Pt
Interest pour Molybdenum carbide
Dispersion in carbon materials

## Slide 5: Context : Hydrogen Evolution Reaction using Mo based materials
J. Liu et al., Metal-doped Mo2C (metal = Fe, Co, Ni, Cu) as catalysts on TiO2 for photocatalytic hydrogen evolution in neutral solution, Chinese J. Catal. 2021, 42, 205
Polarization curves
Tested materials : Mo carbide , M doped Mo carbide M =Fe, Co, Ni, Cu
Direct synthesis of : Mo based materials dispersed in carbon ?
M doped Mo based materials dispersed in carbon ?
Hydrogen production
Stability test (M=Cu)

## Slide 6: Synthesis method : Laser synthesis
Juliette Karpiel
Flame reaction
Nanopowder
Confinement gas
Gas
Liquid and/or gaseous precursors
Carrier gas
CO2 laser
Parameters
- Choice of precursor : composition
- Laser power
-> temperature
-> cristallinity
Reactant flow
-> time of residence
-> size
Advantage :
« continuous » method

## Slide 7: Synthesis method : Laser synthesis
Juliette Karpiel
Flame reaction
Nanopowder
Confinement gas
Gas
Liquid and/or gaseous precursors
Carrier gas
CO2 laser
Temperature :
- Laser Power
- addition of a « sensitizer » gaz
C2H4 : increases temperature
source of Carbon
NH3 : increase temperature
reducing effect
incorporation of N
Choice of precursor : composition
aqueous solution of
(NH4)6Mo7O24.4H2O
This study

## Slide 8: Synthesis method : Laser synthesis
Aerosol of precursors : Pyrosol device
Carrier gas
Precursors
(NH4)6Mo7O24.4H2O +
Ni(acetate) or Ni(nitrate)
Aerosol
Juliette Karpiel
Preparation of precursors (Mo, Ni) suspension
Laser pyrolysis
Annealing
droplets

## Slide 9: Synthesis of Molybdenum carbide
Nano poudre de carbure de molybdène
MOCs | Débit C2H4 (ccm) | Débit NH3(ccm) | Production horaire (mg/h) | % C
15 | 100 | 0 | 397 | 83,52
17 | 100 | 100 | 298 | 70,67
NH3 decreases production rate and C content

## Slide 10: Synthesis of Molybden carbide : STEM and EDX analysis
Crystallized nanoparticles in an amorphous phase
% massique O | % massique N
5,8% | 0,7%
Yellow = molybden
Particles + dispersed Mo

## Slide 11
Chart: 2-theta (deg)
Mo5N6 (cluster precursor) | 1
One oxide MoO2 phase +
two MoC et α-Mo2C
carbide phases
MoO2
MoC
Mo2C
Synthesis of Molybden carbide : DRX

## Slide 12
Echantillons | Dopage | gaz réducteurs | mrécoltée (mg/h) | Produit obtenu (DRX) | Teneur en C (%) | % NI
MOC21 | Non | C2H4 seul | 357 | Mélange MoO2 (mono) + α-Mo2C (hexa) + η-MoC (cub) | 77,15 | 
MOC22 | Non | C2H4 + NH3 | 200 | Mélange MoO2 (mono) + α-Mo2C (hexa) + η-MoC (cub) | 60,87 | 
MOC25 | Nitrate de Ni | C2H4 seul | 275 | Mélange MoO2 (mono) + α-Mo2C (hexa) + η-MoC (cub) | 61,58 | 
MOC26 |  | C2H4 + NH3 | 151,3 | Mélange MoO2 (mono) + α-Mo2C (hexa) + η-MoC (cub) | 45,82 | 
MOC27 | Acétate de Ni | C2H4 seul | 350 | Mélange MoO2 (mono) + α-Mo2C (hexa) + η-MoC (cub) | 70,38 | 
MOC28 |  | C2H4 + NH3 | 156,7 | Mélange MoO2 (mono) + α-Mo2C (hexa) + η-MoC (cub) | 43,89 | 0.55 %
What about Ni « doped » samples ?
Addition of Ni precursor decreases the C content
Ni present in the powder

## Slide 13: Ni « doped » samples : EDX analysis
Ni and Mo appear
co-localized

## Slide 14: Molybdenum carbide : preliminary HER results
The materials are activ ! However some room for improvement…
Doped materials to be tested

## Slide 15: Thank you for attention!

## Slide 16: Molybden carbide : electrochemical measurements (literature)

## Slide 17
2/ Caractérisation des carbures de molybdène par pyrolyse laser.
DRX MOCs :

## Slide 18: Context : HER
O : bleu
Mo : Rouge
C : vert

## Slide 19: Molybden carbide : synthesis methods
Y. Ma et al., Molybdenum carbide as alternative catalyst for hydrogen production – A review, Renew. Sustain. Energy Rev. 2017, 75, 1101.

## Slide 20: Diffraction des rayon x
Présence de deux phases de carbures identifié à 39° et 43° et une phase d’oxyde
Identifié à 26°.
Le rapport des pics indique que le MOC 15 contient plus de d’oxyde que le MOC16

## Slide 21
Echantillons | Réactifs | Dopage | gaz réducteurs | mconsommée (g) | mrécoltée (mg/h) | Produit obtenu (DRX) | Teneur en C (%) | Masse Mo entrainée (g)
MOC21 | AHM+urée | Non | C2H4 seul | 81,0 (mais fuite entre pyrosol et bouteille) | 357 | Mélange MoO2 (mono) + α-Mo2C (hexa) + η-MoC (cub) | 77,15 | 44,0 mais pas possible
MOC22 |  | Non | C2H4 + NH3 |  | 200 | Mélange MoO2 (mono) + α-Mo2C (hexa) + η-MoC (cub) | 60,87 | 
MOC23 |  | Nitrate de Co | C2H4 seul | 16,8 | 364 | Mélange MoO2 (mono) + α-Mo2C (hexa) + η-MoC (cub) | 71,34 | 9,13
MOC24 |  |  | C2H4 + NH3 |  | 167,3 | Mélange MoO2 (mono) + α-Mo2C (hexa) + η-MoC (cub) | 51,86 | 
MOC25 |  | Nitrate de Ni | C2H4 seul | 17,0 | 275 | Mélange MoO2 (mono) + α-Mo2C (hexa) + η-MoC (cub) | 61,58 | 9,24
MOC26 |  |  | C2H4 + NH3 |  | 151,3 | Mélange MoO2 (mono) + α-Mo2C (hexa) + η-MoC (cub) | 45,82 | 
MOC27 |  | Acétate de Ni | C2H4 seul | 14,6 | 350 | Mélange MoO2 (mono) + α-Mo2C (hexa) + η-MoC (cub) | 70,38 | 7,93
MOC28 |  |  | C2H4 + NH3 |  | 156,7 | Mélange MoO2 (mono) + α-Mo2C (hexa) + η-MoC (cub) | 43,89 | 
MOC29 |  | Acétate de Co | C2H4 seul | 17,8 | 339 | Mélange MoO2 (mono) + α-Mo2C (hexa) + η-MoC (cub) | 71,42 | 9,67
MOC30 |  |  | C2H4 + NH3 |  | 150,7 | Mélange MoO2 (mono) + α-Mo2C (hexa) + η-MoC (cub) | 44,85 |