## Slide 1
Role of dimensionality and size in controlling the drag Seebeck coefficient of doped silicon nanostructures.
Raja Sen, Nathalie Vast, Jelena Sjakste
Laboratoire des Solides Irradiés, CNRS, Ecole Polytechnique, CEA/DRF/IRAMIS Institut Polytechnique de Paris, France

## Slide 2
Thermoelectric phonon drag effect
Theoretical framework and implementation
- Effect of SOC and nanostructuring on phonon drag in Si
Outline
2

## Slide 3
Flow of charge carriers (V1 > V2)
V1
Thot
V2
Tcold
Flow of heat (Thot > Tcold)
External perturbation
gradient of temperature/voltage difference
Seebeck coefficient - diffusion & drag
The effect of non-equilibrium phonons and electrons
PHONON DRAG EFFECT
Si: Seebeck vs. Temperature
T. Geballe and G. Hull, Phys. Rev. 98, 940 (1955).
Phonon drag is important even at room temperature
3

## Slide 4
PHONON DRAG EFFECT IN NANOSTRUCTURES ?
Phonon mean free path
Thermal conductivity
Phonon drag effect
K. Fauziah et al., AIP Adv. 10, 075015 (2020).
N. Bennett et al., Appl. Phys. Lett. 107, 013903 (2015).
Is phonon drag effect completely killed at nanoscale?
Only theory can separate drift and drag contributions
4

## Slide 5
Thermoelectric phonon drag effect
Theoretical framework and implementation
- Effect of SOC and nanostructuring on phonon drag in Si
Outline
5

## Slide 6
PHONON DRAG: THEORY
Flow of charge carriers (V1 > V2)
V1
Thot
V2
Tcold
Flow of heat (Thot > Tcold)
Coupled transport equations for electrons and phonons:
6

## Slide 7
PHONON DRAG: THEORY
Coupled transport equations for electrons and phonons:
Out-of-equilibrium phonon population:
Phonon drag term
7

## Slide 8
PHONON DRAG TERM
Paulatto et al. Phys. Rev. B 87, 214303 (2013)
P. Giannozzi, et al., J. Phys. Condens. Matter 21, 395502 (2009)
Poncè et al. Comput. Phys. Commun. 209, 116 (2016)
Implementation into EPW code: Raja Sen
8

## Slide 9
The Seebeck coeff. vs. Temp.
Fiorentini et al. Phys. Rev. B 94, 085204 (2016)
Zhou et al. Proc. Natl. Acad. Sci. USA 112, 14777 (2015)
The Seebeck coeff. vs. Carrier concentration
T. Geballe and G. Hull, Phys. Rev. 98, 940 (1955).
PHONON DRAG IN BULK Si
9
Implementation into EPW code: Raja Sen

## Slide 10
Thermoelectric phonon drag effect
Theoretical framework and implementation
- Effect of SOC and nanostructuring on phonon drag in Si
Outline
10

## Slide 11
PHONON DRAG FOR HOLES in Si: SOC
Zhou et al. Proc. Natl. Acad. Sci. USA 112, 14777 (2015)
SOC improves theory/experiment agreement
Band structure changes (effective mass)
11
R. Sen, N. Vast, and J. Sjakste, Phys. Rev. B 108, L060301 (2023)

## Slide 12
PHONON DRAG IN Si NANOSTRUCTURES
At 100 nm, phonon drag still not completely quenched
in thin films and nanowires for in-plane transport
Geometry and direction dependence
Direction-dependent Casimir model:
300 K
12
R. Sen, N. Vast, and J. Sjakste, Phys. Rev. B 108, L060301 (2023)

## Slide 13
PHONON DRAG IN Si NANOSTRUCTURES
At 100 nm, phonon drag still not completely quenched
in thin films and nanowires for in-plane transport:
expected to increase at lower T
300 K
13
R. Sen, N. Vast, and J. Sjakste, Phys. Rev. B 108, L060301 (2023)

## Slide 14
PHONON DRAG IN Si NANOSTRUCTURES
R. Sen, N. Vast, and J. Sjakste, Phys. Rev. B 108, L060301 (2023)
At 100 nm, phonon drag still not completely quenched
Agreement with experiment. But caution!
K. Fauziah et al., AIP Adv. 10, 075015 (2020).
N. Bennett et al., Appl. Phys. Lett. 107, 013903 (2015).
300 K
Geometry and direction dependence
14

## Slide 15
Conclusion
Direction-dependent phonon drag term implemented into EPW code
Spin-orbit coupling plays important role for hole phonon drag in Si
At 100 nm, phonon drag still not completely quenched in thin films and nanowires for in-plane transport direction at 300 K.
Calculations help to disentangle phonon drag effect from other ones

## Slide 16
Thank you for your attention!

## Slide 17: Phonon-drag in Silicon nanostructures:
Only zone centered acoustical phonons are responsible for the phonon-drag Seebeck.
q: phonon momentum
Jacoboni et al. Rev. Mod. Phys. 55, 645 (1983)
C. Herring. Phys. Rev. 96, 1163 (1954)

## Slide 18: Ab initio study of transport coefficients:
Linearized Boltzmann transport equation (BTE) in steady-state:
Electronic distribution function in presence of small electric field E and gradient of T:
where the collision integral reads:
Conductivity:
Thermopower:
We implemented the response of the distribution function with respect to into the EPW code.

## Slide 19: Electron-phonon scattering process:
The carrier-phonon scattering integral can be expressed as:
where the scattering rate reads:
Schematic representation of the four phonon-assisted scattering processes:
Poncé et al. Rep. Prog. Phys. 83, 036501 (2020)

## Slide 20: Electron-impurity scattering process:
The carrier-impurity scattering integral can be expressed as:
with
Under the Brooks and Herring model can be written as:
and the reciprocal of the screening length () can be written as:
We implemented the impurity scattering model into the EPW code.
Fiorentini et al. Phys. Rev. 94, 085204 (2016)
Jacoboni et al. Rev. Mod. Phys. 55, 645 (1983)

## Slide 21: Interpolation of electron-phonon matrix element:
Coarse k/q mesh
W90
MLWF
MLWF
Dense k/q mesh
Real Space
Sjakste et al. Phys. Rev. B 92, 054307 (2015)
Giustino et al. Phys. Rev. B 76, 165108 (2007)
Verdi et al. Phys. Rev. Lett. 115, 176401 (2015)
Bloch to Real space (Fourier transform.)
Real to Bloch space
(Inverse Fourier transform.)