## Slide 1: PHONON TRANSPORT IN ASYMMETRIC NANOSTRUCTURES IN THE QUASI-BALLISTIC REGIME
GDR NAME plenary days, 2023 Rennes
Boris Brisuda, Institut Néel, Cnrs
Thesis Supervisors: Olivier Bourgeois and laurent saminadayar

## Slide 2: Phonon physics at low temperatures
Umklapp scattering, phonon inclusions
Ballistic transport
Long phonon mean free path
Fully diffusive phonon transport
Quantum behaviours
Phononic crystals
Boundary scattering, size limited phonon transport (Casimir/Ziman)
Heat manipulation through phonon engineering  thermal metamaterials
Objectives:
  Coherent effects, quantization of thermal conductance
  Phononic crystals
  Thermal rectification
Absolute Zero
300 K
Notes: Introduce phonon physics, phonon engineering, and our objectives of study. Why low temperature is interesting

## Slide 3: Phonon characteristic lengths at low temperatures
Dominant wavelength
  with m/s
Mean free path
  Average distance between two inelastic collisions
  Sample length  ballistic transport
  ;
  at very low temperatures  boundary limited

## Slide 4: Suspended SiN thermal bridge sensor
20 µm
  Mechanically suspended for thermal isolation
  NbN thermometer and Au heater for reversible measurement
  Suspended nanostructured strip
40 steps in fabrication process
  Resist spinning
  Lithography
  Deposition
  Lift-off
  Etching
1 month minimum
Heaters
Thermometers
2 µm
5 µm

## Slide 5: Measurement setup
NbN sample holder thermometer calibration
Nguyen, T., Tavakoli, A., Triqueneaux, S. et al. Niobium Nitride Thin Films for Very Low Temperature Resistive Thermometry. J Low Temp Phys 197, 348–356 (2019). https://doi.org/10.1007/s10909-019-02222-6

## Slide 6: Measurement of BB38
  3 membranes per measurement campaign
    1 single membrane setup
    1 thermal bridge setup
  Thermometer calibration
    Saturation below 100 - 150 mK
  Heating and measurement of the membranes done by the thermometers !
    DC current used for heat dissipation through the thermometer and low AC current used to measure its resistance
    Sub-optimal, risk of decoupling electrons from phonon bath below 100 mK

## Slide 7: Single membrane setup
Fixed temperature bath T0
  Fixed probe current IAC
  Apply ramping heating current IDC = f(T0)
  Measure the increased T1 for each IDC
T0
T0

## Slide 8: Single membrane setup
Fixed temperature bath T0
  Fixed probe current IAC
  Apply ramping heating current IDC = f(T0)
  Measure the increased T1 for each IDC
For small
  We can obtain (T)

## Slide 9: Single membrane setup
Fixed temperature bath T0
  Fixed probe current IAC
  Apply ramping heating current IDC = f(T0)
  Measure the increased T1 for each IDC
  Repeat for different T0
For small
  We can obtain (T)
For high T1, size limited transport (Casimir/Ziman)
  Mean free path defined only by system dimension

## Slide 10: Single membrane results
(Casimir)
Temperature

## Slide 11: Thermal bridge setup
Fixed temperature bath T0
  Fixed probe current IAC on both sides
  Apply ramping heating current IDC = f(T0) on one side (a)
  Measure the increased and for each IDC
  Repeat for different T0
  Repeat by heating on side (b)
Using the measured from single membrane setup
a side
b side
a --> b
a <-- b
b
a
a --> b
a <-- b
a
b
300 nm
200 nm
260 nm
1 µm
5 µm

## Slide 12: Thermal bridge results
a  b
For T0 = 300 mK - 1 K
b  a
For T0 = 300 mK - 1 K

## Slide 13: Thermal rectification
Definition of rectification factor used in this work:
a side
b side
a --> b
a <-- b
1 µm
for T0 = 400 mK
for T0 = 400 mK

## Slide 14: Thermal rectification factor
Rectification factor
Rectification factor for

## Slide 15: Conclusion
  Fabrication of suspended membranes
  First measurement at dilution fridge temperatures
  Rectification observed in asymmetric SiN strips
  More data treatment necessary
  Measurements of different samples

## Slide 16: Acknowledgments
ANR HANIBAL
  CEA – Natalio Mingo, Carlos Polanco-Garcia
  IEMN - Jean-François Robillard, Jon Canosa-Diaz
TPS team and technical support of Institut Néel
  Olivier Bourgeois and Laurent Saminadayar
  Thierry Crozes and Pierre Gasner for the fabrication support
  Victor Doebele
Lancaster university

## Slide 17: Thank you for your attention !

## Slide 18: Preliminary results
Ballistic transport Heat flux symmetry
A. Tavakoli et al. Nat. Commun. 9, 4287 (2018)

## Slide 19: Preliminary results
Probing of rectification through mass asymmetry
A. Tavakoli, J. Maire, B. Brisuda et al. Sci Rep 12, 7788 (2022)

## Slide 20: Non-Fourier transport regimes

## Slide 21: Radiation vs Joule heating
Joule heating
Radiation
Radiation with shielding
  With shield, radiation reduced by 90%

## Slide 22: Noise estimation

## Slide 23: Kapitza and electron phonon coupling
W/K
and
W/K

## Slide 24: Electron-phonon coupling constant
Silicon nitride sample phonons,
Electrons,
Phonons,
NbN thin film
Temperature (mK)
Resistance
Puissance/Volume (

## Slide 25: Setup issues
Rectification
  Lack of time reversal asymmetry
  Lack of non-linearity ???
Measurement
  Membrane temperature inhomogeneity
    Below 100mK
    Simulation neglecting several sources of scattering
C.A. Polanco, A. van Roekeghem, B. Brisuda, L. Saminadayar, O. Bourgeois, and N. Mingo, The phonon quantum of thermal conductance: are simulations and measurements estimating the same quantity?, Sci. Adv. 9, 2023

## Slide 26: Beams SiN
  is the specific heat related to phonons carrying heat only
For large SiN microwires as measured by Tavakoli, @1K
  W/m/K
For our experiment :
W/m/K
W/K

## Slide 28: Strip
  (
with
W/K

## Slide 29: Beams NbTi
Resistance of contact leads = difference between normal state and superconductive state
  
  W/K
Nb supra W/K

## Slide 30: Overetching

## Slide 31
SiN membrane phonons,
Electrons,
Phonons,
NbN thin film thermometer
Surrounding heat bath,
T1
T0
T0