## Slide 1: Preparation of 3D electrodes for microsupercapacitors by spin-coating
N. Poirot, M. Gabard, M. Boufnichel, R.Omnée , E. Raymundo-Piñero
Journées Plénières GDR NAME 2023, Rennes, November 8th-10th 2023

## Slide 2
Energy storage devices: Key technology for the development of energy autonomous systems
Industrial areas
  Photovoltaics, micro-sensors, robotics, electronic components, memory circuits, portable devices (computers, phones), portable medical devices, IoT, etc.
Current objective: energy microsources: microbatteries, microsupercapacitors (MSC)
3D structuration: Superior performance / planar technology
3D Si-based micro-LIB / MSC energy storage systems
  High specific surface area
  High energy/power density
  Type of structuration depends on the final use of the 3D systems
Context
Experimental
TiO2 coating
Conclusion
*Ragone plot comparing the energy and power densities of various state-of-art supercapacitors and batteries with ASCs
*Choudhary et al. Adv. Mater. 2017, 29, 1605336
**YUE et al. Front. Mech. Eng. 2017, 12(4): 459–476
**Applications of different Li-ion battery energy storage systems
3D-electrodes performances

## Slide 3
W. Zheng et al. J. of Power Sources 341 (2017), doi.org/10.1016/j.jpowsour.2016.11.093
Increasing of specific capacity with AEF (*8)
Na2SO4 electrolyte
0,07 mF/cm2 à 20 mF/cm2
Si nanowires (Metal assisted anodic etching (MAAE))
23.6 SiNW2
7.4 SiNW1
3D-Microsupercapacitor
Context
Experimental
TiO2 coating
Conclusion
3D-electrodes performances

## Slide 4
Challenge
  Active material conformal deposition by liquid route on the 3D template high aspect ratio
Ours objectives
  Preparation of 3D electrodes : sol-gel and spin-coating techniques
  Easy to implement, fast and low-cost method compared to techniques as PVD, ALD, CVD,…
Ellis et al., Adv. Mater., 26, 3368–3397, (2014)
Context
Experimental
TiO2 coating
Conclusion
3D-electrodes performances
Notes: On s’est inspiré des travaux de Li. Ils élaborent des films TiO2 avec du noir de carbone sur des feuilles d’aluminium pour une application de photocatalyse. Ti butoxide précurseur de Ti, solvent propanol et acétylacétone et eau pour l’hydrolyse

## Slide 5
Gravure Bosch process
**Eustache et al., Adv. Energy Mater., vol.4, 1301612 (2014)
*Baggetto et al., Adv. Energy Mater., vol.18, p. 1057-1066 (2008)
Topology | Aspect Ratio | Etched Depth µm | Width µm | Spacing µm | Footprint Length cm | h µm | ν µm | Area Enlargement Factor (AEF)
*Trenches | 9 | 52 | 6 | 3 | 0.7 | - | - | 12.6
Trenches | 29 | 117 | 4 | 3 | 0.7 | - |  | 34.4
**Pillars | 29 | 144 | 5 | - | - | 9 | 8 | 32.4
TiO2 coating
Conclusion
3D-electrodes performances
Context
Dimensions and area enlargement factor
6 mm
3 mm
142 mm
125 mm
8,4 mm
8,5 mm
2,2 mm
2,3 mm
Experimental

## Slide 6
Active material deposition on Si-3D substrates
Oxide precursors, solvant, complexant,…
Deposition by spin coating of (Sol + PE)
Impregnation of 3D substrate
Thermical decomposition on hot plates
Polymerisation of resin
Preparation sol
Oxide crystallisation by RTA
Patent A.Vincent, N. Poirot, WO 2015\044582 Al (2015)
Patent « Réalisation de microbatteries 3D par voie liquide », M. Gabard, N. Poirot, F. Ghamouss, T. Tillocher, N°1000376145 (2016)
Patent « Dépôt conforme par voie liquide sur topologie 3D », N. Poirot, N° 1000409098 (2017)
M. Gabard, M. Zaghrioui, D. Chouteau, V. Grimal, T. Tillocher, F. Ghamouss, N. Poirot, ChemEngineering 1(1), 5 (2017)
TiO2 coating
Conclusion
3D-electrodes performances
Context
Experimental
PE resin

## Slide 7
Process steps of capillary coating
Evolution monitoring of the polymer solution in temperature (camera)
Pore ​​filling, spin coating
TiO2 coating
Conclusion
3D-electrodes performances
Context
Removal
Low internal constraints
Experimental
Polymerization at room temperature

## Slide 8
Thermal decomposition after 40 min
Strong internal constraints
Preferential fracture zone
Process steps of capillary coating
TiO2 coating
Conclusion
3D-electrodes performances
Context
Experimental
N. Poirot, T. Tillocher, and P.I. Raynal, “Conformal coating by liquid route on three-dimensional topology” Eur. Phys. J. Spec. Top. (2022)

## Slide 9
LaNiO3 oxide: metal electrode, MIM capacitor
TiO2 coating
Conclusion
3D-electrodes performances
Context
Experimental
1 mm
1 mm
100 nm
100 nm
30 nm
35 nm
70 nm
25 nm
Plots
H=32 mm, L= 3 mm
FF = 10
Layer thickness : 30 nm
Conformal coating

## Slide 10
TiO2 thin layers on Si-2D substrates
  Optimal thickness of the active material layer
  Optimal electrochemical performance
100 nm
20 nm
40 nm
60 nm
120 nm
200 nm
200 nm
90 nm
100 nm
100 nm
100 nm
100 nm
200 nm
300 nm
Film thickness
  by adding coating layers
  by varying the precursor solution concentration
Homogeneous TiO2 films without cracks and fissures
Good adhesion
TiO2 coating
Conclusion
3D-electrodes performances
Context
Experimental
N. Poirot, M. Gabard, M. Boufnichel, R. Omnée, Encarnacion Raymundo-Piñero, “A suistainable approach for the development of TiO2 based 3D electrodes for micro-supercapacitors”, Batteries 2023,9, 258.

## Slide 11
Electrochemical characterization on 2D-Si electrodes – TiO2
  *Electrolyte: 1 M LiPF6 (EC:PC:3DMC); Ti/Si/TiO2 (PVD)
Surface capacitance at different current densities vs. film thickness*
Nyquist plot withTiO2 thicknesses of 200 nm or 120 nm
TiO2 coating
TiO2 layer : thickness of 120 nm selected to be deposited over 3D supports having high surface areas for optimal performance.
Conclusion
3D-electrodes performances
Context
Experimental
Optimum surface capacitance : 120 nm
For 200 nm : low electrical conductivity

## Slide 12
Coating on 3D trenches
AR 9 AR 29
TiO2 coating
Conclusion
3D-electrodes performances
Context
Experimental
50 µm
10 µm
top
2 µm
117 µm
10 µm
Layer thickness 110 nm
bottom

## Slide 13
Coating on 3D pillars with AR 29
TiO2 coating
Conclusion
3D-electrodes performances
Context
Experimental
Thickness
130 nm
200 nm
bottom
Detail of a pillar wall
Details of bottom pillar
  Advantages
  Low cost
  Simple, easy (clean room not required)
  Deposit covering the walls of the structure
  Controlled microstructure and thickness of the active layer
144 µm

## Slide 14
Conclusion
3D-electrodes performances
Context
Experimental
Cyclic voltammogramms at 1 mV.s-1 of 2D and 3D AR 29 TiO2 electrodes (120 nm)
  Faradic and capacitive contribution with different OR waves at the same potentials : TiO2 has the same structure in two morphologies
Surface capacity at different current densities for electrodes 2D et 3D
  Trenches topology more efficient
  Improvement in the energy and the power density : requirements of a supercapacitor
TiO2 coating

## Slide 15
Surface capacity at different current densities for electrodes with a layer of 120 nm of TiO2
Experimental and theoretical surface capacitances obtained against the surface AEF -Trenches
Conclusion
3D-electrodes performances
Context
Experimental
TiO2 coating
Current Density mA cm−2 | Surface Capacitance mF.cm−2 |  |  | 
 | 2D | 3D AR9 Trenches | 3D AR29 Trenches | 3D AR29 Pillars
0.01 | 8.1 | 46.5 | 85.0 | 73.7
0.05 | 2.4 | 22.7 | 60.8 | 38.4
0.1 | 1.6 | 16.5 | 51.9 | 23.9
0.2 | 1.0 | 10.5 | 42.5 | 9.0
0.3 | 0.7 | 7.5 | 36.6 | 2.3
0.5 | 0.4 | 5.3 | 28.8 | 0.2
Current Density mA cm−2 | Surface Capacitance mF.cm−2 |  |  | 
 | 2D | 3D AR9 Trenches | 3D AR29 Trenches | 3D AR29 Pillars
0.01 | 8.1 | 46.5 | 85.0 | 73.7
0.05 | 2.4 | 22.7 | 60.8 | 38.4
0.1 | 1.6 | 16.5 | 51.9 | 23.9
0.2 | 1.0 | 10.5 | 42.5 | 9.0
0.3 | 0.7 | 7.5 | 36.6 | 2.3
0.5 | 0.4 | 5.3 | 28.8 | 0.2
Trenches topology more efficient
Quality of TiO2/Si interface
Perfect correlation
Contribution of surface capacitive
Performance proportional to the 3D specific surface
Exp
Theo.

## Slide 16
  Simple method to implement
  Feasibility of liquid deposition on 3D Si substrates with different aspect ratios
  The thickness of the active material layers : solution concentration and the number of layers
  Homogenous TiO2 thin film coating on 3D substrates : uniformly covers the walls, top and bottom
    For trenches (AEF 34) : surface capacitance of 85.0 mF cm−2 (0,01mA cm−2)
    At 0.5 mA cm−2 : 69-fold increase in the surface capacitance : capacitance value of 28.8 mF cm−2
  Method for depositing oxide for high AEF efficient for developing high-energy and high-power devices.
  Others applications : SOFC, photovoltaic, ferroelectric, MIM capacitor,…
Context
Experimental
TiO2 coating
3D-electrodes performances
Conclusion

## Slide 17
GREMAN
  A. Vincent, T. Defforge, G. Gautier, V. Grimal, M. Gabard, S. Desplobain, D. Chouteau
Collaborations
  Thomas Tillocher, GREMI Orléans
  E. Raymundo, R. Omnée, CEMHTI, Orléans
  Zaid Abdelali, StMicroelectronics-Tours : réalisation de condensateurs MIM
  Mohamed Boufnichel, Morgane Dutour, StMicroelectronics-Tours : gravure Si
Région Centre Val de Loire
Programme Lavoisier/CEA
ANR
Acknowledgments
Thanks for your attention
1 mm
2 mm